- DATA

| Glass Fiber Complex 1080 |  |
| --- | --- |
| Glass composition | E-CR Glass |
| Weight per unit area (Deviation from the nominal value) | 1075 g/m² ± 8 % |
| 1st layer: Chopped Strand Mat | 500 g/m² |
| 2nd layer: Woven Roving |  |
| Warp 0° | 150 g/m² |
| Weft 90° | 410 g/m² |
| Bonding | Stitching |
| Sewing thread polyester | ≤ 15 g/m² |
| Moisture content | < 0.15 % |
| Edges | Trimmed |
| Width* (Deviation from the nominal value) | Variable ± 1.5 cm |
| Type of size | Suitable for UP-, VE- and EP- resins |
| Coupling agent | Silane |
| Tube diameter, internal | 70 mm |

* Other roll widths, tube diameters, and lengths available on request.

- PROCESSING / STORAGE

The product should be conditioned for 24 hours at room temperature in the application area prior to use. Store in its original packaging and keep dry. Storage temperature should not exceed 35°C.

- DELIVERY FORM

Rolls are packed in stretch film and supplied on pallets.

The information in this data sheet corresponds to our knowledge and experiences at the present time. The information does not constitute legally binding assurance of properties. Before you use the product, check this on its suitability. Since the processing are beyond our control, it is subject solely to user.