PRODUCT DESCRIPTION

Lateral Repairs Connection Liner is a flexible and versatile solution for the rehabilitation of non-pressure pipelines, designed to restore lateral connections with precision and reliability. Manufactured from a durable polyester knitted hose with a thermoplastic coating, it is available in sizes ranging from DN50 to DN300, with 45°, 90°, and 180° connection options.

This proven system is engineered to adapt to a wide range of installation conditions, providing contractors with a dependable solution for junction rehabilitation. For projects requiring unique specifications, custom sizes can also be supplied in consultation with Lateral Repairs.

Lateral Repairs Connection Liners combine strength, adaptability, and ease of use, making them a trusted solution for extending the service life of pipeline infrastructure.

TECHNICAL DATA

| Product name | Stitched and Sealed Connection Liners |  |
| --- | --- | --- |
| Delivery Status | Material Data | ISO Test Method |
| Weight | Approx. 450 g/m² | DIN EN 29073 T1 |
| Thickness With Coating | Approx. 3.0 mm | DIN EN 29073 T2 |
| Pore Volume | Approx. 85 % |  |
| Fibers | Polyester |  |
| Coating | TPU; PUR |  |
| Coating Thickness | Approx. 150 μm |  |
| Seam Type | Stitched and sealed |  |
| Curing | Ambient, Hot Water, Steam Mix |  |
| Properties | DN50 to DN300 45°, 90°, 180° connections * Other angles available on request. |  |

| Product name | Stitched (Not Sealed) Connection Liners |  |
| --- | --- | --- |
| Delivery Status | Material Data | ISO Test Method |
| Weight | Approx. 450 g/m² | DIN EN 29073 T1 |
| Thickness With Coating | Approx. 3.0 mm | DIN EN 29073 T2 |
| Pore Volume | Approx. 85 % |  |
| Fibers | Polyester |  |
| Coating | TPU; PUR |  |
| Coating Thickness | Approx. 150 μm |  |
| Seam Type | Stitched |  |
| Curing | Ambient, Hot Water, Steam Mix |  |
| Properties | DN50 to DN300 45°, 90°, 180° connections * Other angles available on request. |  |